Certificate of Analysis

General properties:

Name：PLGA15000-PEG5000-MAL, PLGA:75/25

Molecular Weight：20150 Dalton

Cat.#： R-P-105015

Lot.#： RP201604011

Manufacture Date： 2016.04.11

Date of Analysis： 2016.04.11

Recommended Retest date： 2017.04.11

Stability： 12 months

Storage： -20°C in the dark

Structure

| Items | Specification | Results |
| --- | --- | --- |
| Appearance | White/ Off-white solid | White solid |
| 1H NMR | Identical to the Structure | Identical to the Structure |
| Foreign Material | None | None |
| Substitution | ＞90% | 92% |
| PDI |  | <1.3 |

Report Date: 2016.04.11

This product is for research use only, Not for human or animal use